Technical Data Sheet

1 / 3 pages

Thermal Conductivity

Silicone elastomer

FEATURES

-Thermal Conductivity

Silicone Rubber

BENEFITS

- Excellent thermal conductivity

- Excellent flame retardancy ability

COMPOSITION

- Silicone polymer

- Thermally conductive filler

SH6280U

1. Product Description

SH6280U is thermal conductivity silicone rubber for compression molding/extruding which can be used for parts of electronic, electric and computer etc that are getting hotter when working

2. Applications

Thermally conductive sheet, cap, tube etc.

3. Key Performance Properties

- Thermal conductivity is excellent

- Flame retardancy property is excellent (UL 94V-0, E253047)

- Roll workability is good

4. Typical properties

| Properties | Test method | Unit |  | SH6280U |
| --- | --- | --- | --- | --- |
| Appearance | ASTM E1767 | - |  | Dark grey |
| Williams plasticity | ASTM D926 | - |  | 280 |
|  | Curing agent | - | 1) KC-8 | 2) KC-2 |
|  | Amounts | phr | 0.5 phr | 1.2 phr |
| Curing condition |  |  |  |  |
|  | Press 1st cure | - | 10mins, 170℃ | 5mins, 120℃ |
|  | Oven 2nd cure | - | 4hrs, 200℃ | 4hrs, 200℃ |
| Specific gravity | ASTM D792 | - | 2.17 | 2.17 |
| Hardness | ASTM D2240 | Shore A | 80 | 80 |
| Tensile strength | ASTM D412 | MPa | 4.0 | 4.2 |
| Elongation | ASTM D412 | % | 100 | 66 |
| Tear strength | ASTM D624 C | N/㎜ | 9.0 | 11 |
| Linear shrinkage | JIS K6249 | % | 2.8 | 2.3 |
| Thermal | ASTM D5470 | W/m.K | 1.0 | 1.0 |
| conductivity |  |  |  |  |
| Flame retardancy | UL-94 |  | V-0 | V-0 |

- KC-8 : 2,5-dimethyl 2,5-di(t-butyl peroxy) hexane 45 % paste

- KC-2 : 2,4-dichlorobenzoyl peroxide 50% paste

- Typical properties should not be used as specifications

They are evaluated in laboratory, and can be different from test condition.

Technical Data Sheet

| Thermal Conductivity | SH6280U |
| --- | --- |
| Silicone elastomer |  |

5. How to use

2 / 3 pages

For blending or coloring, milling with two-roll mill is the most suitable process. Milling time should be carefully decided to secure uniformity of materials.

6. Limitation

The featured product must be checked prior to use.

- If applying to other purposes, defects can be generated.

- If using non-suggested curing agents, its own properties can be altered.

- If mixing with other products, degradation of properties and defects can be caused.

- Additives or pigments must be used under technical support of KCC.

- If it's first use, product must be applied after technical suggestion and assistance of KCC.

Any other inquiries or methods of use can be found on KCC webpage and enquired

technical support team at KCC.

7. Handling Precautions

- Wear eye protection and protective gloves when handling this product.

- Curing reaction in room temperature may occur when mixing with a product which has polymer with hydrogen functional group without retarder. This phenomenon cannot be limited to our product. It can be occurred when mixing with other companies' products.

8. Safety and Storage

- Use it within 12 months from the date of manufacture.

- Keep out of the reach of the children.

- During transportation, try to avoid direct sunlight. Conditions of under 30℃

with shade is commended.

- If store condition is not fulfilled, the products' lifetime may be affected. Also, deterioration of the products' quality within shelf life time may occur.

Technical Data Sheet

| Thermal Conductivity | SH6280U |
| --- | --- |
| Silicone elastomer |  |

3 / 3 pages

9. Packaging

20 kg box

10. Warranty Information – Please read carefully

This TDS is considered to be accurate. KCC's guarantee of the product will apply, only if conditions on TDS (limitation, notice, application) are fulfilled within expiry date. If not, KCC cannot guarantee the quality of the product.

KCC’s sole warranty is that the product will meet the KCC sales specifications in effect at the time of shipment. Your exclusive remedy for breach of such warranty is limited to replacement of any product shown to be other than as warranted.

KCC specifically disclaims any other express or implied warranty of fitness for a particular purpose or merchantability. Unless KCC provides you with a specific, duly signed endorsement of fitness for use, KCC disclaims liability for any incidental or consequential damages.

Suggestions of use shall not be taken as inducements to infringe any patent.

11. The date of issue

The first date of issue : 2009.03.01

The revised date of issue : 2015.08.01 (3rd)

- Please refer to MSDS if you want to know more specific usage or caution.

For further information, please visit our website, www.kccsilicone.co.kr.